Extended macroscopic description 
of non-wetting liquid intrusion into a ball of porous material

Tomasz Czerwiński, Mieczysław Cieszko, Eugeniusz Czapla

Institute of Mechanics and Applied Computer Science, Kazimierz Wielki University,

Kopernika 1 St. 85-074 Bydgoszcz, e-mail: thhomekcz@gmail.com, cieszko@ukw.edu.pl

Abstract

The problem of macroscopic description of quasi static intrusion of non-wetting liquid (mercury) into a ball of porous material is considered. Modelling of these processes is of great importance for interpretation of the mercury intrusion curves used for determination of the pore size distribution and other pore structure parameters of porous materials. For interpretation of such curves the simplified microscopic models of the pore space structure are applied that do not take into account the shape and size of the investigated sample and therefore lead to significant faults. Application of the macroscopic description of mercury intrusion is a new approach to this problem allowing avoiding these faults in interpretation of the experimental data.

A new macroscopic description is proposed for quasi static process of non-wetting liquid intrusion into a ball of porous material. The analysed problem is an extension of the description presented in the paper [1]. Considerations are based on the continuum model of the capillary transport of liquid and gas in unsaturated porous materials, proposed by one of authors of the present paper [2]. The key assumptions of this model are: division of liquid in the pore space into two macroscopic constituents called mobile liquid and capillary liquid; description of menisci motion by an additional macroscopic velocity field; parametrization of saturation changes by a macroscopic pressure-like quantity that for quasi static and stationary processes is equal to the capillary pressure. We assume that at the beginning of the intrusion process pressure of mercury is equal to zero and the ball pore space is empty (Fig. 1). This process is stopped when all pores of the ball are fulfilled with mercury.

Fig.1. Scheme of quasi static intrusion of a non-wetting liquid into a ball of porous material

This process is described by equation for saturation distribution with the mobile liquid. In the spherical coordinate system this equation takes the form

(1)

where by  saturation of the ball with the mobile and capillary liquid are denoted, respectively,  stand for the pressure,  are coefficients characterize processes of the capillary transport in the pore space of porous material.

References

Cieszko M., Czapla E., Kempiński M.: Continuum Description of Quasi-Static Intrusion of Non-Wetting Liquid into a Porous Body, Continuum Mechanics and Thermodynamics 27(1), 133-144, 2015.

Cieszko M.: Macroscopic Description of Capillary Transport of Liquid and Gas in Unsaturated Porous Materials, Meccanica 22, 1-22, 2016.